POLYMER BASED HYBRID MICROGELS: CLASSIFICATION, DEVELOPMENT, CHARACTERIZATION AND BIOMEDICAL APPLICATIONS

(Review Article)

*Malik Naveed1, 2, Khizar Hayat2, 3 Muhammad Jamil1

1Institute of Chemistry, University of the Punjab, Lahore, Pakistan

2Department of Chemistry, Minhaj University, Lahore, Pakistan

Department of Chemistry, Quid-e-Azam University, Islamabad

Corresponding Author address: maliknavy@gmail.com Cell #: +92313-6445436

ABSTRACT: This review is reported about the classification, advancement in method of synthesis and characterization. Various methods are there for the synthesis of hybrid microgels of required properties. Characterizations of these multifunctional materials are given with special reference to vibrational, scattering and imaging techniques. Special application with respect to biomedical applications is also focused shortly.

Keywords: Hybrid microgels, X-rays Diffraction, Drug Delivery,

INTRODUCTION

Gels: are three dimensional cross linked structures, with a unique property of swelling when placed in some proper solvent media (lyogel). When the solvent media is aqueous then they are known as hydrogel [1]. Gels obtained from of biological systems are agarose, carrageenan, gelatin, pectin, and agar [2, 3]. Fibrin clots is another biological gels, which are comprises of fibrinogen monomer produced by series of enzymatic polymerization reactions [4]. Some synthetic organic systems shows the properties of gels at certain temperature and concentration, for example, very dilute solution of polyvinylchloride in di(2-ethylhexyl) phthalate become gels on decrease in temperature [5]. Styrene-divinyl benzene copolymer swollen in some organic solvent [6] and a 2-hydroxyethyl methacrylate ethylene glycol dimethacrylate copolymer become gel in water [7, 8]. Silica gel is an example of inorganic gel in swollen state [9, 10].

Microgels: Microgels are also cross linked three dimensional colloidal structures having size within the range of 100 nm to 5 µm [11, 12] in the swollen state. Shrinked microgels are within the range of 1nm-100 nm [13] having dispersive property in solvent [14]. Microgels are very sensitive toward external environmental stimuli like temperature [15], pH [16], salt content in the media [17], electromagnetic field [18], nature of the solvent [19], electrolytic concentration [20], sugar content [21], osmotic pressure [22] and some metal like Pb [23] and K [24]. Most widely studied microgels till now is poly(N-isopropylacrylamide), which shows changed in volume with change in temperature [25].

Hybrid Microgels: Now days a new class of microgels has been introduced known as hybrid microgels synthesized by loading inorganic nanoparticles into microgels [26]. Interesting functional hybrid microgels are prepared by combining organic polymer with the inorganic part such as Quantum dots [27], Ag [28], magnetic particles (Fe2O3) [29] and Au [30]. There is symbiotic relationship between organic and inorganic part in hybrid microgels in which organic part (microgels) maintain colloidal nature and the inorganic part imparts optical properties like photoluminescence [31] or surface plasmon resonance [32] to the hybrid microgels. Gold nanoparticles, with different shape have been synthesized, such as platelets [33], polyhedrons [34] spheres [35], rods [36] and multipods [37].

CLASSIFICATION OF HYBRID MICROGELS

Physically Cross-linked Microgels: In physically cross-linked microgels, network formation are occurs due to Van der Waal’s forces of attraction, for example, hydrophobic [38] or ionic interactions [39]. Physically cross-linked microgels are mostly used for the encapsulation of drugs which are released on dissolution of the polymer layer network. Physically crosslinked microgels largely depend on some factors, like polymer composition, ionic strength of medium and temperature. Physically crosslinked microgels are usually synthesis from biopolymers and their typical examples include alginate [40], carrageenan [41], dextran and agarose [42].

Chemically Cross Linked Microgels: Chemically crosslinked microgels are somewhat more stable than their physically crosslinked counterparts due to covalent nature. Covalently crosslinked microgels are typically synthesis by copolymerizing monomers in the presence of a multifunctional crosslinking agent. For example, poly (2-hydroxyethyl methacrylate) is a widely studied microgel synthesized from 2-hydroxy methacrylate with ethylene glycol dimethacrylate [43].

Thermo-responsive Microgels: Microgels that give response on slight change in temperature are thermo-responsive microgels. Polymer poly(N, N’-diethylacrylamide) [44], poly(N-isopropylacrylamide) [45], 3-poly(N-isopropyl acrylamide/acrylamide) [46], and poly(N-isopropylacrylamide- co-acrylic acid) are behaved as thermo-responsive polymer [47]. Thermo-responsive microgels exhibit a significant change in volume at the volume phase transition temperature [48]. Temperature above the lower critical solution temperature (LCST), the microgels particles present in shrinked form, and below the LCST, they turned into hydrophilic and become swell. This property of microgels makes them more attractive for their application in controlled drug release and diagnosis.

pH Responsive Microgels: Microgels that can response on slight change in pH are pH responsive microgels. Various examples reported in the literature are poly(acrylic acid)/poly(vinyl amine) (PAAc/PVAm) [49], poly(methyl methacrylate-co-methacrylic acid) [P(MMA-co-MAA)] [50], poly(2-vinylpyridine) (P2VP) [51], and poly[2-(diethylamino) ethyl methacrylate] (PDEA) [52].

Salt Responsive Microgels: The microgels having ability to respond against salt concentration are salt-responsive microgels. Hydrodynamic radii of the hybrid microgels largely depend upon type and electrolyte concentration. Electrolytes affect the hydrodynamic radius, colloidal stabilization and zeta potential of microgels. It was observed that hydrodynamic radius decreases with increasing ionic strength of electrolyte in the dispersion medium [53].

Multi-Responsive Microgels: Multi responsive microgels give response against two or more than two stimuli at the same time. Microgels showing Dual-response toward external stimuli are usually PNIPAM-based for example poly(N-isopropylacrylamide-co-acrylic acid) P(NIPAM-co-AAc) can respond against temperature and pH [54]. Poly-[2-(N-morpholino) ethylmethacrylate] microgels can response to external temperature, salt concentration, stimuli including pH and organic solvents. poly-[2-(N-morpholino)ethylmethacrylate] microgels can interact with electromagnetic field of Fe3O4 magnetic particles [55].

Electrical Signal Sensitive Microgels: Microgels showing change in their volume in the presence of applied electric field is known as electric signal responsive microgels [56]. Chitosan based gels are mostly used in electrically modulated drug delivery.

Light Sensitive Microgels. These gels are very sensitive toward light, and undergo change in volume on light exposure. These gels are widely used in cartilage tissue engineering [57] and photo-responsive artificial muscles [58].

Hybrid microgels can be classified based on type of polymerization during the synthesis, organic material used like N-isopropylacrylamide (NIPAM), acrylic acid (AA) and N-vinylcaprolactam (VCL), inorganic material as gold, platinum, silver, palladium, zinc oxide, iron oxide, cadmium telluride and cadmium selenide nanoparticles as inorganic part. Properties and applications are another base to classify the hybrid microgels like the magnetic, photoluminescent and plasmonic properties [59].

SYNTHESIS OF MICROGELS

Synthesis of microgels can be divided into different classes on the basis of mechanism. Mostly the microgels are synthesized by emulsification methods.

Microgels Formed by Homogeneous Nucleation. In this method soluble monomer are polymerized in simple round bottom flask by adding some cross linking agent. Over the course of polymerization the microgels appear as insoluble polymer. Poly N-isopropylacrylamide can be synthesis by using this method because it is insoluble in water. Polacrylamide cannot be prepared by this method by homogeneous nucleation as it swell to give macrogels. Following types of polymerization occurs via homogeneous nucleation

- Surfactant free emulsion polymerization

- Emulsion polymerization

Surfactant Free Emulsion Polymerization: Thermo-responsive hybrid microgels are usually prepared via surfactant free emulsion polymerization microgels and are prepared by simple temperature controlled magnetic stirring of monomer along with oxidizing agent without the use of any surfactants. Typically, the reactor is feed with monomer, water, surfactant and radical initiator soluble in water. The monomer is initially present in the form of suspended drop, whereas at the end of the polymerization process the polymer is obtained stabilized particles [60, 61].

Inverse Emulsion Polymerization: Water in oil emulsion system is used in this process. In inverse polymerization polymerized microgels obtained in emulsion form which is then precipitated from organic liquid [62].

Core–Shell Type Microgels Preparation: Thermosensitive core shell microgels were first synthesized by Makino [62]. Core–shell latex nanoparticles prepared by emulsion polymerization have been available. The core particles are first prepared via emulsion polymerization. There are a number of problems in the synthesis of core–shell microgels particles. Firstly, uniform seed generation nucleation controlled. That is, synthesis of uniform core–shell particles, stage-2 polymer chains should be deposit on existing particles, avoiding secondary nucleation of stage-2 particles. Secondary nucleation of stage-2 polymer is a major problem. EM technique is commonly used for the identification of secondary nucleation. Usually secondary stage nucleation involves more population of particle around larger core-shell polymer. Another challenge involves rearrangement of core–shell particles into more complex appearance. For example, preparation of core shell particles with more hydrophobic shell is very difficult.

Synthesis of Hybrid Microgels: Different methods are now been used for the synthesis of hybrid microgels. Metal NPs are mostly prepared by chemical or photo reduction [63], chemical reduction with the help of radiation [64], microwave-assisted synthesis and thermal decomposition [65]. Silver fabricated poly (N-isopropylacrylamide-co-acrylic acid) (poly (NIPAAm-co-AAc)) are synthesized by using NaBH4 as a reducant [66]. As Poly (N-isopropylacrylamide) (PNIPAAm) is biocompatible, aqueous soluble with very low cytotoxicity [67]. These properties make them very important in biomedical application.

Organic-inorganic hybrid microgels containing Au fabricated into the poly-NIPAAm-co-allylacetic acid have been prepared. Experimental data shows that the allylacetic acid enhanced the temperature sensitivity of the microgel. The Au NRs used change the behavior of fabricated polymer like poly(styrene ulfonate)/poly(allylamine hydrochloride) with layer-by-layer polyelectrolyte [68].

Emulsion Polymerization: It is actually a radical polymerization in which emulsion comprises of water, monomer and surfactant, is stir for particular time at specific temperature. Emulsion polymerization extensively used to encapsulate different kinds of inorganic nanoparticles. Process involves encapsulation of metal oxide in polystyrene [69]. Emulsion polymerization method has a disadvantage known as the diffusion processes so this polymerization process is not usually used for the encapsulation of nanoparticles into the matrix of microgel. However, batch emulsion polymerization used to incorporate, macro-monomer, co-monomers and the synthesized polymer particles [70].

Mini-emulsion Polymerization: In Mini-emulsion polymerization, two separate phases are vigorously stirred as shown in figure 1.

In order to obtain polymer of micron, two phases consist water insoluble monomer and aqueous phase containing surfactant. The initiator used can be water soluble. The large surface area of the very small droplets increases ability particles to capture radical produced during the polymerization by the initiator.

Figure 1: Diagrammatic explanation of mini-emulsion polymerization [70]

Till now various inorganic particles have been incorporated into microgels through mini-emulsion polymerization like TiO2 [71] and ZnO [72]. In water in oil (w/o) polymerization or inverse micro-emulsion process the droplets of w/o micro-emulsions are in the form of tiny compartments known as “nano-reactors”. Deng prepared different variety of particle by using micro-emulsion polymerization [70]. Now days this technique is widely applied for the preparation of nanoparticles [71], metal oxide [72] and complex material [73].

Encapsulation of Inorganic Parts into Microgels: Incorporation of inorganic nanoparticles is usually carried out by emulsion or precipitation polymerization. In this method covalent bond is usually formed between nanoparticles and microgels. For encapsulation generally polymerization techniques followed is like to encapsulation of silica and gold. Encapsulation of inorganic particle into the microgels occurred during the above mention method of hybrid microgels polymerization. Inorganic particle can also be incorporated into the microgels by following physical method.

Physical Encapsulation: Physical encapsulation may occur through polymer adsorption and layer by layer assembly. It involves single or multilayer adsorption of charged inorganic particle (charged seed) on the counter charged polyelectrolytes. Main purpose of the method is to entrap the inorganic particle into polymer shell layer. In this type of encapsulation physical interaction is there in between the two component of hybrid microgel. This interaction may be created due to the presence of polar functional group in the polymer like thiol group present in Glutathione. Physical interaction may be ion pairing, complexation and dipole-dipole interaction [74].

Figure 2: Encapsulation of nanoparticles via layer-by-layer (LBL) assembly [75]

Polymerization after Adsorption on Seed: This newly developed method was first described by the Furusawa in 1999 and prepared to load inorganic particles into the core of cationic sensitive PNIPAAm. This technique involved the encapsulation of inorganic part through adsorption on seeded organic polymer part that is actually electrostatic force of interaction between two parts [75, 76].

Double Emulsion like Process: This oil in water in oil (o/w/o) has been extensively used for encapsulating iron oxide particles into polymer. It involves synthesis in oil phase in organic solvent water either through oil in water in oil system [77] or water in oil in water system [78]. Compatibility point of view encapsulation of inorganic particles, dispersed in inorganic media and hydrophobic nanoparticles in organic media having organic polymer matrix. Bodmeir introduced the method of water in oil in water encapsulation techniques as shown in figure 3 [79].

Figure 3: w/o/w emulsion like process [80]

CHARACTERIZATION OF HYBRID MICROGELS

Various characterization techniques are used for the determination of particle size, shape and the morphological study of hybrid microgels.

UV-Visible Spectroscopy: Hybrid microgels absorb UV-Visible region light because of resonance oscillation originated at the interface polymer matrix and nanoparticles in fact due to a surface plasmon resonance (SPR) phenomenon. As the every microgel containing nanoparticles exhibits surface plasmon resonance highly dependent upon pH and temperature.

Surface Plasmon Resonance property of hybrid microgels used to evaluate the kinetics of loading of nanoparticles in the matrix of organic polymer and important one is the study of volume phase transition of hybrid microgels; decider of when and how much hybrid microgels would unload. Change in volume phase transition highly dependent upon the gap between the nanoparticles and polymer within the matrix, which ultimately depend upon the pH and temperature [81].

Fourier Transform Infrared (FTIR) Spectroscopy Functional groups of the microgels are determined by the FTIR spectroscopy. This technique also confirms the successful interaction between the nanoparticles and microgels as after the incorporation of nanoparticles into the matrix of microgels spectra recorded again. Fourier Transform Infrared (FT-IR) spectra is very effective tool to predict the molecular structure of microgels and the strength of interaction between inorganic nanoparticles and microgels as the bond frequency highly effected by the interaction between the two parts [81, 82].

Thermogravimetric Analysis: Thermal analysis is for the study of different parameter like phase transition temperature, adsorption and desorption nature of the hybrid microgels,  thermal degradation, type and extent of grafting in the microgels, extent of polymerization, loading of nanoparticles in the microgels and percentage purity of hybrid microgels along with extent of water in the microgels.

X-Rays Diffraction analysis (XRD): Characterization, purity, structure and presence of inorganic nanoparticles are confirmed by XRD analysis as the each particular inorganic component gives specific intensity signal [83] i.e. Bragg reflection at 2θ from which particle size determined using Debye-Scherrer formula [84]. Crosslinking and percentage composition is determined with advanced technique known as energy dispersive XRD.

Electron Microscopy (EM): Morphological study as well as interior surface of the hybrid microgels studied by high resolution technologies likes scanning electron microscopy and transmission electron microscopy. Some of the very important physical properties are studied are shape, size, appearance and polydispersity. As these properties greatly dependent upon the method hybrid microgels preparations and the condition given to the method, it highly helpful to decide what method should followed to prepare the particular range of particles [85]. Current emerging application of TEM is reported to be used to study the swelling and de-swelling behavior of core-shell microgels [86].

Atomic Force Microscopy: Specialty of this amazing technology is to give 3 dimensional views with high resolution, cross-sectional analysis, to give images of collapsed hybrid microgels, samples in solution form and now volume phase transitions of hybrid microgels are study using this technique [86].

Dynamic Light Scattering: Most demanding property of hybrid microgels is its hydrodynamic study which is highly dependent on pH, sugar content and temperature. Extent of change in volume that is swelling and de-swelling determined by scattering method i.e. angle of scattering. The size, size distribution, hydrodynamic diameter and determined with the help of dynamic light scattering (DLS). It can be of following types.

- Angular dependent photon correlation spectroscopy

- Photon correlation spectroscopy (PCS)

Light scattering goniometer is commonly used for angular dependent photon correlation spectroscopy. At fixed scattering angle of θ = 60 at λ = 661.8 nm, swelling curves were appeared. The measurement is taken thermal equilibrium of the solution. PCS is used to determine the hydrodynamic functionality of microgels [87]. All the thermal dependent measurements are taken at a fixed scattering angle of 600. The hydrodynamic radius can be calculated by using Stokes- Einstein equation:

Rh=kbT/ 6πητq-2

Where q = 4πn/λsin⁡(θ2)  is the magnitude of the scattering vector, kBT is the thermal energy, η is viscosity and n is the refractive index of the solvent [88, 90].

BIOMEDICAL APPLICATIONS

Hybrid microgels containing inorganic nanoparticles are widely used in different field of biochemistry and biotechnology. Hybrid microgels sensitive to photo-thermal stimuli also have interestingly uses in drug delivery. Some hybrid microgels containing dyes as nanoparticles are responsible for photosensitivity [91, 92] a basic requirements for imaging. For a polymer to be photosensitive should have resonance wavelength in between 800 nm-1200 nm. This range is known as water window as it can penetrate through body tissue [93]. Hybrid microgels extensively used in vitro as well as vivo diagnostic purpose likes bio-separation, immobilization of biomolecules, purification etc. and in therapeutic application. Therapeutic application involves the drug delivery, bio-imaging and targeted treatment of cancer cells [94]. Inorganic nanoparticles such as ZnO, Ag, Au, and quantum dots are widely used. Hybrid microgels shows, optical, magnetic, electronic, and catalytic properties [95]. Iron oxide containing microgels have supra magnetic properties which make them to be very effective in the separation of biomolecules and it acts as simple and rapid responsive carrier hence can be used for the coupling of biomolecules. SPION (supra paramagnetic iron oxide nanoparticles) are acts as excellent carriers for biomolecules (antibodies, proteins, antigens etc.) for in vitro diagnostic field, in purification and separation of these molecules as probe for RNA/DNA hybridization & identification [96]. One of the most interesting applications of hybrid microgels is their uses as biosensors like sensing of glucose. Currently, hybrid microgels used in the determination glucose as glucose indicator in the biomedical field because the glucose monitoring is very important for healthy life [97]. Hybrid microgels have been successfully loaded with glucose oxidase via electrochemical method [98]. Hybrid microgels containing targeted drug, release on change in temperature, pH and ionic strength [99-102]. This also was used to control the loading and release polymer molecules [103-105]. Salt-triggered sensitivity of hybrid microgels promises to become a very easy, effective and important for the loading and release of sensitive macromolecules as well as drug such as amino acids, enzymes and DNA in micro containers [74, 106-107].

CONCLUSION

Different method of synthesis of hybrid microgel and their current modern characterization enable us to synthesis of hybrid microgel of our interest functionalities, including their morphology, shape, response ability, size and loading of inorganic particles into the matrix of organic part. Extent and target release of loaded drug from hybrid microgels is largely controlled by method of preparation and procedure follow for the loading of drug into the microgels. The major problem faced to process synthesis of hybrid microgels is the incompatibility of inorganic part (metal or metal oxide) with organic polymer part. Currently hybrid microgels gained huge application in the different field like controlled drug delivery, cell imaging and treatment of target cell especially cancer cell. Hybrid microgels are extensively used in specific nucleic acid capture, immunoassay, cell sorting and in various biotechnological applications.

REFERENCES

- Burchard, W. Macrogels, “Microgels and Reversible Gels-What is difference”. Polym. Bull. 58(1): 3-14(2007)

- Clark, A.H., Ross-Murphy, S.B. “Structure and mechanical properties of biopolymer gels”. Biopolymer. 83: 157-192(1987)

- Burchard, W., Ross-Murphy, S.B. “Physical Networks:  Polymers and Gels”. London, UK, 1990

- Ferry, J.D. “Structure and rheology of fibrin networks: In biological and synthetic polymer networks”. London, UK. 41-55 (1988)

- Te, K. “Viscoelastic properties of thermo-reversible gels. In Physical Networks: Polymers and Gels”. London, UK: 15-33(1990)

- Staudinger, H., Husemann, E., Uber hochpolymere Verbindungen.  Deut. Chem. Ges: 68, 1618-1634 (1935)

- Wichterlee, O.; Lim, D. “Hydrophilic Gels for Biological Use”. Nature. 185, 117-118(1960)

- Refojo, M.F. “Contact lenses”. Kirk-Othmer Encycl. Chem. Techn. 3rd edn, 720-742(1979)

- Graham, T.J. “On the properties of silicic acid and other analogous colloidal substance”.  Chem.  Soc.  Lond. 17, 318-27(1864)

- Hermans, P.H. Gels. In Colloid Science, Vol. II, ed. H.R. Kruyt. Elsevier publishing company, Inc.; Amsterdam, The Netherlands. 483-651(1949)

- Pelton, R. “Temperature sensitive aquous microgels”. Adv. Colloid. Interf. Sci. 85, 1-33(2000)

- Meng, Z.; Smith, M.H.; Lyon, L. “Temperature programmed synthesis of micron sized multi-responsive microgels”. Colloid. Polym. Sci. 287(3), 277-285(2009)

- Pollack, G.H. Cells, Gels, and the Engines of Life, Ebner and Sons, Seattle, WA USA. 2001

- Paul C.H.; Raj. R. “Principles of Colloid and Surface Chemistry”. 3rd edn, revised and expanded, CRC Press. 1997

#### Xu, S.; Zhang, J.; Kumacheva, E. “Hybrid polymer-inorganic materials: multiscale hierarchy”. Comp. Interf. 10(4-5), 405-421(2003)

- Giovanni, N.; Munch, J.P.; Candau, S.J. “Swelling, Structure and Elasticity of Polyampholyte Hydrogels. Langmuir, 15, 4236-4244(1999)

- López-León, T., Elaïssari, A., Ortega-Vinuesa, J.L., Bastos-González, D. “Hofmeister effects on poly(NIPAM) microgel particles: macroscopic evidence of ion adsorption and changes in water structure”. Chemphyschem, 8(1), 148-156(2007)

- Suzuki, D.; Kawaguchi, H. “Modification of gold nanoparticle composite nanostructure using thermo-sensitive core-shell particles as a template”. Langmuir, 21(18), 8175-8179(2005)

# Molina, M.J., Gomez-Anton, M.R., Pierola, I.F. “Determination of the parameters controlling swelling of chemically cross-linked pH-sensitive poly (N-vinylimidazole) hydrogels”. J. Phy. Chem B. 111(42), 12066-12074(2007)

- Park, T.G., Hoffman, A.S. “Sodium chloride induced phase transition in nonionic poly(N-isopropylacrylamide) gels”. Macromolecules, 26(19), 5045–5048(2993)

# Zenkl, G., Mayr, T., Khmant, I. “Sugar-Responsive Fluorescent Nanosphere”. Macromol. Biosci. 8(2), 146–152(2008)

# Bradley, M., Garcia-Risueño, B.S. Symmetric and asymmetric adsorption of pH responsive gold nanoparticles onto microgel particles characterization”. J. Colloid. Interf. Sci. 355, 321–327(2011)

- Luo, Q., Guan, Y., Zhang, Y., Siddiq, M. “Lead sensitive PNIPAM microgels modified with crown ether group”. J. Polym. Sci. Part A: Polym. Chem. 48(11), 4120–4127(2010)

- Ju, X.J., Liu, L., Xie, R., Niu, C.H., Chu, L.Y. “Dual thermo-responsive and ion-recognizable monodisperse microsphere”. Polymer, 50(3), 922–929(2009)

# Pelton, R. “Temperature-sensitive aqueous microgels”.  Adv. Colloid. Interf. Sci, 85(1), 1–33(2000)

- Karg, M., Hellweg, T. “New” smart” poly (NIPAM) microgels and nanoparticles microgels hybrids: properties and advances in characterization”. Curr. Opin. Colloid. Interf. Sci, 14(6), 438–450(2009)

- Janczewski, D., Tomczak, N., Han, M.Y., Vancso, G.J. “Stimulus responsive PNIPAM/QD hydrid microspheres by copolymerization with surface engineered QDs”. Macromolecules, 42(6), 1801–1804(2009)

## Xu, H., Xu, J., Zhu, Z., Liu, H., Liu, S. “In-situ formation of silver nanoparticles with tunable spatial distribution at the poly (N-isoprpylacrylamide) corona of unimolecular micelles”. Macromolecules, 39(24), 8451–8455(2006)

# Luo, B., Jie-Song, X., Zhang, F., Ao, X., Wang, C., Hu, J.J., Chang-Chun, W. “Multi-functional thermo-sensitive composite microspheres with high magnetic susceptibility based on magnetite colloidal nanoparticle clusters”. Langmuir, 26(3), 1674–1679(2010)

# Kawano, T., Niidome, Y., Mori, T., Katayama, Y., Niidome, T. “PNIPAM gel-coated nanorods for targeted delivery responding to a near-infrared laser”. Bioconjugate Chem, 20(2), 209–212(2009)

## Bai, S., Wu, C., Gawlitza, K., Klitzing, R.V., Marion, B., Ansorge-Schumacher., Wang, D. “Using hydrogels microparticles to transfer hydrophilic nanoparticles and enzymes to organic madia via stepwise solvent exchange”. Langmuir, 26(15), 12980–12987(2010)

- Karg, M., Lu,Y., Carbo-Argibay, E., Pastoriza-Santos, I., Perez-Juste, J., Liz-Marzan, L.M., Hellweg, T. “Multi-responsive hybrid colloids based on gold nanorods and poly (NIPAM-co-allylacetic acid) microgels: temperature and pH tunable plasmon resonance”. Langmuir, 25(5), 3163–3167(2009)

- Lofton, C.; Sigmund, W. Mechanism controlling crystal habits of gold and silver colloids. Colloids. Adv. Funct. Mater, 15, 1197–1208(2005)

- Kim, F., Connor, S., Song, H., Kuykendall, T., Yang, P. “Platonic gold nanocrystals”. Angew. Chem, 116(28), 3759–3763(2004)

- Liz-Marzan, L. M., Giersig, M., Mulvaney, P. “Synthesis of nanosized gold-silica core-shell particles”. Langmuir, 12(18), 4329–4335(1996)

- Pastoriza-Santos, I., PMrez-Juste, J., Liz-MarzKn, L.M. “Silica-coating and hydrophobation of CTAB-stablized gold nanorods”. Chem. Mater, 18(10), 2465–2467(2006)

- Nehl, C.L., Liao, H., Hafner, J.H. “Optical properties of star shaped gold nanoparticles”. Nano Lett. 6(4), 683–688(2005)

- Omari, A., Chauveteau, G., Tabary, R. “Gelation of polymer solution under shear flow”. Colloid. Surf. Physicochem. Eng. Asp. 225(1), 37-48(2003)

- Ouwerx, C., Velings, N., Mestdagh, M.M., Axelos, M.A.V. “Physico-chemical properties and reology of aliginate gel beads formed with various divalent cation”. Polym. Gel. Net. 6, 393-408(1998)

- Kuo, S.M., Niu, G.C., Chang, S.J., Kuo, C.H., Bair, M.S. “A one-step method for fabricating chitosan microspheres”. J. App. Polym. Sci. 94(5), 2150-2157(2004)

- Ortiz, J., Aguilera, J.M. “Effect of Kappa-Carrageenan on the gelation of horse Mackerel (T. Murphi) raw paste surimi-type”.  Food Sci. Tech. Intr. 10, 223-232(2004)

- Bulone, D., Biagio, P.L.S. “Mesoscopic gel at low agarose concentration in water: a dynamic light scattering study”. Biophysical Journal. 68(4), 1569-1573(1995)

- Eichenbaum, G.M.P., Kiser, F., Dobrynin, A.V., Simon, S.A., Needham, D. “Investigation of the swelling response and loading of ionic microgels with drugs and protein: The dependence on cross-link density”. Macromolecules. 32(15), 4867-4878(1990)

- Freitag, R., Panayitou, M., Pohner, C., Vandevyver, C., Wandrey, C., Hilbrig, F. “Synthesis and characterization of thermo-responsive poly(N, N’-diethylacrylamide) microgels.” React. Funct. Polym. 67(9), 807–819(2007)

- Pelton, R. “Temperature-sensitive aquous microgels”. Adv. Colloid. Interf. Sci. 85(1), 1-33(2000)

- Liang, B.R., Zhang, Q.S., Zha, L.S., Ma, J.H.J. “Synthesis and characterization of novel, temperature sensitive microgels based on N-isopropylacrylamide and tert-butyl acrylate”. Appl. Polym. Sci. 103(5), 2962–2967(2007)

- Fernandez-Barbero, A., Capriles-Gonzalez, D., Sierra-Martin, B., Fernandez-Nievest, A. “Coupled Desewelling of Multiresponsive Microgels”. J. Phys. Chem. B. 112, 12195–12200(2008)

- Loxley, A., Vincent, B. “Equilibrium and kinetic aspects of the pH-dependent swelling of poly (2-vinylpyridine-co-styrene) microgels”. Colloid. Polym. Sci. 275(12), 1108–1114(1997)

- Liang, B.R., Zhang, Q.S., Zha, L.S., Ma, J.H. “Synthesis and characterization of novel, temperature sensitive microgels based on N-isopropylacrylamide and tert-butyl acrylate”. J. Appl. Polym. Sci. 103, 2962–2967(2007)

- Saunders, B.R., Crowther, H.M., Vincent, B. “Poly [(methyl methacrylate)-co-(methacrylic acid)] microgel particles: swelling control using pH, cononsolvency and osmotic deswelling”. Macromolecules, 30(3), 482-487(1997)

- Tanaka, K., Fillmore, D. “Kinetics of swelling of gels”. J. Chem. Phys. 70(3), 1214–1218(1979)

- Peppas, N.A., Marek, S.R., Conn, C.A. “Cationic nanogels based on diethylaminoethyl mathacrylate”. Polymer, 51(16), 1237–1243(2010)

- Zha, L., Hu, J., Wang, C., Fu, S., Elaissari, A., Zhang, Y. “Preparation and characterization of poly (N-isopropylacrylamide-co-dimethylaminoethyl) microgel latexes”. Colloid. Poly. Sci. 280(1), 1–6(2002)

- Zha, L.S., Zhang, Q.S., Ma, J.H., Liang, B.R. “A novel route to prepare pH and temperature-sensitive nanogels via a semibatch process.” J. Colloid. Inter.  Sci. 330(2), 330–336(2009)

- Vural, B., Ahmet, A., Cansel, T., Yasemin, B. “novel multiresponsive microgels: Synthesis and characterization studies.” Langmuir, 27(20), 12657–12665(2011)

- Ramanathan, S., Block, L.H. “The use of chitosan gels as matrices for electrically-modulated drug delivery.” J. Control. Release. 70(1), 109-123(2001)

- Anseth, K.S., Metters, A.T., Bryant, S.J., Martens, P. J., Elisseeff, J. H.; Bowman, C. N. “In situ forming degradable networks and their application in tissue engineering and drug delivery.” J. Control. Release. 78(1), 199-209(2002)

- Qiu, Y., Park, K. “Environment-sensitive hydrogels for drug delivery.” Adv. Drug. Deliv. Rev. 53(3), 321-339(2001)

- Cao, Z., Du, T., Chen, T., Nie, J., Xu, J., Fan, F. “Preparation and properties of thermo-sensitive organic/inorganic hybrid microgels.” Langmuir. 24(22), 12771(2008)

- Aslam, K., Ahmed, M.E., Salman, A., Mohamad, A., Mansour, A., Abdullah S.A. “Microwave-assisted synthesis of silver nanoparticles using poly-N-isopropylacrylamide/acrylic acid microgel particles”. Colloid. Surf. A: Physicochem. Eng. Aspects. 377(1), 356–360(2011)

- Lei, J., Shuqing, S., Shiyuan, C., Jianjun, Y., Huan, L., Xiaoqing, L. “Microgel-silica hybrid particles: Strategies for tunable nanostructure, composition, surface property and porphyrin functionalization”. J. Colloid. Inter. Sci. 348(2), 408–415(2010)

- Makino, K., Yamanoto, S., Fujimoto, K., Kawaguchi, H., Oshima, H. “Surface Structure of latex particles covered with temperature-sensitive hydrogel layers.” J. Colloid. Interf. Sci. 166(1), 251-258(1994)

- Socol, Y., Abramson, O., Gedanken, A., Meshorer, Y., Berenstein, L., Zaban, A. “Suspensive electrode formation in pulsed sonoelectrochemical synthesis of silver nanoparticles”. Langmuir. 18, 4736–4740(2002)

- Xia, L.H., Zhou, R.M., Gracien, E.B., Francis, A. O. “Synthesis of silver nanopartilces by EB irradiation”. J. Radiat. Res. Radiat. Process, 22, 69–72(2004)

- Shiraishi, Y., Toshima, N. “Colloidal silver catalysts for oxidation of ethylene”. J. Mol. Catal. A: Chem. 141(1), 187–192(1999)

- Dong, Y., Ma, Y., Zhai, T., Shen, F., Zeng, Y., Fu, H., Yao, J. “Silver nanoparticles stabilized by thermoresponsive microgel particles: synthesis and evidence of an electron donor–acceptor effect”. Macromol. Rapid Commun. 28(24), 2339–2345(2007)

- Ankareddi, I., Bailey, M.M., Brazel, C.S., Rasco, J.F., Hood, R.D. “Developmental toxicity assessment of thermoresponsive poly(N-isopropylacrylamideco-acrylamide) oligomers in CD-1 mice”. Birth. Defects.Res.83(2), 112–116(2008)

- Karg, M., Lu, Y., Carbo-Argibay, E., Pastoriza-Santos, I., Perez-Juste, J., Liz-Marzan, L.M., Hellweg, T. “Multiresponsive hybrid colloids based on gold nanorods and poly (NIPAM-co-allylacetic acid) microgels: temperature and pH tunable plasmon resonance.” Langmuir, 25(5), 3163–3167(2009)

- Daniel, J.C., Schuppiser, J.L., Tricot, M. “Magnetic polymer latex and preparation process”. 1982

- Tuncel, D., Demir, H.V. “Conjugated polymer nanoparticles.” Nanoscale, 2(4), 484–494(2010)

- Al-Ghamdi, G.H., Sudol, E. D., Dimonie, V.L., El-Aasser, M.S. “Encapsulation of titanium dioxide in styrene/n-butyl acrylate copolymer by miniemulsion polymerization”. J. Appl. Polym. Sci. 101(5), 3479–3486(2006)

- Kobitskaya, E., Ekinci, D., Manzke, A., Plettl, A., Wiedwald, U., Ziemann, P., Biskupek, J., Kaiser, U., Ziener, U., Landfester, K. “Narrowly size distributed zinc-containing poly (acrylamide) latexes via inverse miniemulsion polymerization.” Macromolecules. 43(7), 3294–3305(2010)

- Montagne, F., Mondain-Monval, O., Pichot, C., Elaissari, A. “Highly magnetic latexes from submicrometer oil in water ferrofluid emulsion.” J. Polym. Sci. Part. Polym. Chem. 44(8), 2642–2656(2006)

- Yunlu, D., Ping’an, M., Ziyong, C., Xiaojiao, K., Xiao, Z., Zhiyao, H., Chunxia, L., Dongmei, Y., Xuefeng, Z., Jun, L. “Up-conversion cell imaging and pH induced thermally controlled drug release from NaYF4: Yb3+/Er3+@ hydrogel core shell hybrid microspheres”. Nano. 6(4), 3327–3338(2012)

- Rachid, L., Ahmad, B., Mohamed, M.E., Hatem, F., Yannick, M., Ronan, L.D., Abdelhamid, E. “Polymer encapsulation of inorganic nanoparticles for biomedical application”. Int. J. Pharm. 2013

- Montagne, F., Mondain-Monval, O., Pichot, C., Elaissari, A. “Highly magnetic latexes from submicrometer oil in water ferrofluid emulsion.” J. Polym. Sci. Part. Polym. Chem. 44(8), 2642–2656(2006)

- Fromherz, P. “Electrical interfacing of nerve cells and semiconductor chips.” Chemphyschem. 3(3), 276–284(2002)

- Georgieva, D., Schmitt, V., Leal-Calderon, F., Langevin, D. “On the possible role of surface elasticity in emulsion stability.” Langmuir. 25(10), 5565–5573(2009)

- Alex, R., Bodmeier, R. “Encapsulation of water-soluble-drugs by a modified solvent evaporation on drug entrapment.” J. Microencapsul. 7(3), 347–355(1990)

- Ahmed, N., Fessi, H., Elaissari, A. “Theranostic application of nanoparticles in cancer.” Drug Discov. Today. 17(17), 928–934(2012)

- Yun-Yun, L., Xiao-Yun, L., Jian-Mao, Y., Dan-Li, L., Xiao, C., Liu-Sheng, Z. “Investigation of Ag nanoparticles loading temperature responsive hybrid microgels and their temperature controlled catalytic activity.” Colloids and Surfaces A: Physicochem. Eng. Aspects. 393, 105– 110(2012)

- Mirkin, C. A. “Programming the assembly of two-and- three-dimensional architectures with DNA and nanoscale inorganic building blocks.” Inorg. Chem. 39(11), 2258–2272(2000)

- Tianyou, C., Zheng, C., Xiaolei, G., Jingjing, N., Junting, X., Zhiqiang, F., Binyang, D. “Preparation and characterization of thermosensitive organic-inorganic hybrid microgels with functional Fe3O4 nanoparticles as crosslinker.” Polymer. 52(1), 172-179(2011)

- Yun-Yun, L., Xiao-Yun, L., Jian-Mao, Y., Dan-Li, L., Xiao, C., Liu-Sheng, Z. “Investigation of Ag nanoparticles loading temperature responsive hybrid microgels and their temperature controlled catalytic activity.” Colloids and Surfaces A: Physicochem. Eng. Aspects. 393, 105– 110(2012)

- Guoqiang, L., Changling, Z., Jun, X., Yan, X., Tingting, Y., Jing, L., Lei, S., Zhiguang, G., Weimin, L. “Thermo-responsive hollow silica microgels with controlled drug release properties.” Colloids and Surfaces B: Biointerfaces. 111, 7– 14(2013)

- Crassous, J.J., Ballauff, M., Drechsler, M., Schmidt, J., Talmon, Y. “Imaging the volume transition in thermo-sensitive core-shell particles by cry-transmission electron microscopy.” Langmuir. 22(6), 2403–2406(2006)

- Höfl, S., Zitzler, L., Hellweg, T., Herminghaus, S., Mugele, F. “Volume phase transition of “smart” microgels in bulk solution and adsorbed at an interface: a combined AFM, dynamic light and small angle neutron scattering study.” Polymer. 48(1), 245–254(2007)

- Tianyou, C., Zheng, C., Xiaolei, G., Jingjing, N., Junting, X., Zhiqiang, F., Binyang D. “Preparation and characterization of thermo-sensitive organic-inorganic hybrid microgels with functional Fe3O4 nanoparticles as crosslinker.”  Polymer. 52(1), 172-179(2011)

- Pelton, R., Pelton, H.M., Morphesis, A., Rowell, R.L. “Particles sizes and electrophoretic mobilities of poly (N-isopropylacrylamide) latex.” Langmuir. 5(3), 816-818(1989)

- Zeiser, M., Freudensprung., Hellweg T. “Linearity thermo-responsive core-shell microgels: towards a new class of nanoactuators.” Polymer. 53(26), 6096-6101(2012)

- Ivan, G., Lora, M.F., Eugenia, K. “Hybrid Microgels Photosensitive in the near infrared spectral region”. J. Am. Chem. Soc. 126(49), 15938-15939(2004)

- Berry, C.C. Nanobiotechnol. Inorg. Nanopart. vs Org. Nanopart. 4, 159(2012)

- Reese, C.E., Mikhonin, A.V., Kamenjicki, M., Tikhonov, A., Asher, S.A. “Nanogel nanosecond photonic crystal optical switching.” J. American. Chem. Soci. 126(5), 1493-1496(2004)

- Wang, C., Flynn, N.T., Langer, R. “Controlled structure and properties of thermoresponsive nanoparticles-hydrogel composite.” Advanced Materials. 16(13), 1074-1079(2004)

- Zhu, M.Q., Wang, L.Q., Exarhos, G.J., Li, A.D.Q. “Thermosensitive gold nanoparticles.” J.  American. Chemi. Soci. 126(9), 2656-2657(2004)

- Nolan, C.M., Reyes, C.D., Debord, J.D., Garcia, A.J., Lyon, L.A. “Phase transition behavior protein adsorption and cell adhesion resistance of poly (ethylene glycol) cross-linked microgels particles.” Biomacromolecules. 6(4), 2032-2039(2005)

- Macková, H., Horák, D.l., Trachtová, T., Rittich, B., Panová, A. “The use of magnetic poly (N-isopropylacrylamide) microspheres for separation of DNA from probiotic dairy products.” J. Colloid Sci. Biotechnol. 1(2), 235–240(2012)

- Ladj, R., Bitar, A., Eissaa, E., Fessi, H., Mugnier, Y., Dantecb, R. L., Elaissari, A. Int. J. Pharm. 440, 1-12(2013)

- McCowen, K.C., Malhotra, A., Bistrian, B.R. “Stress-induced hyperglycemia”. Crit. Care. Clin. 17(1), 107-124(2001)

- Retama, R., Lopez-Ruizb J.B., Lopez-Cabarcos E. “Microstructural modification induced by the entrapped glucose oxidase in cross-linked polyacrylamide microgels used as glucose sensors.” Biomaterials. 24(27), 2965-2973(2003)

- Wu, W., Shen, J., Li, Y., Zhu, H., Banerjee, P., Zhou, S. “Specific glucose-to-SPR signal transduction at physiological pH by molecularly imprinted responsive hybrid microgels.” Biomaterials. 33(29), 7115-7125(2012)

- De-Geest, B.G., Sanders, N.N., Sukhorukov, G. B, Demeester, J., De Smedt, S.C. “Release mechanism for polyelectrolyte capsules”. Chem. Soc. Rev. 36(4), 636–649(2007)

- Sukhorukov, G., Dahne, L., Hartmann, J., Donath, E., Mohwald, H. “Controlled precipitation of dyes into hollow polyelectrolyte capsules based on colloids and biocolloids”. Adv. Mater. 12(2), 112–115(2000)

- Mendelsohn, J.D., Barrett, C.J., Chan, V.V., Pal, A.J., Mayes, A.M., Rubner, M.F. “Fabrication of microporous thin films from polyelectrolyte multilayers”. Langmuir. 16(11), 5017–5023(2000)

- Tao X., Li, J.B., Mohwald, H. “Self-assembly, optical behavior and permeability of a novel capsule based on an azo dye and polyelectrolytes”. J. Chem. Eur. 10(14), 3397–3403(2004)

- Tokarev, I., Tokareva, I., Minko, S. “Gold nanoparticles enhanced plasmonic effects in a responsive polymer gel”. Adv. Mater. 20(14), 2730–2734(2008)

- Lu, Z.H., Prouty, M.D., Guo, Z.H., Golub, V. O., Kumar, C., Lvov, Y. M. “Magnetic switch of permeability for polyelectrolyte microcapsules embedded with Co@ Au nanoparticles”. Langmuir. 21(5), 2042–2050(2005)